## Slide 1
Alternatives to Ordered phases
At Zero temperature
Meigan Aronson
Stewart Blusson Quantum Matter Institute
Department of Physics and AStronomy
University of British COlumbia

## Slide 2
Jannis Maiwald
Dalmau Reig i Plessis
Xi Yang Li
Meigan Aronson
Alannah Hallas
???
Hallas and Aronson Joint Group
Quantum Materials Discovery Lab
Graham Johnstone
TBD
Joern Bannies

## Slide 3
Interacting Conduction Electrons

## Slide 4: Electronic Interactions: Ordering of Charge and Spin
Coulomb interactions in
(low density) electron gas
Candido 2004
Increasing electron density
Localization of electron charge: Wigner lattice
Minimize potential energy by maximizing distance between electrons.
Spatial ordering of electron spin: ferromagnetic order (polarized fluid)
Peeters 2009

## Slide 5
Magnetic, localized
Nonmagnetic, superconducting
Transitional: depends on compound
Origin of Interactions: Partially filled d- and f- shells in Elements
(after J. L. Smith 1985)
Most neutral atoms in the gas phase have partially filled shells, hence magnetic moments.
Initially, strong hybridization of d- and f- orbitals into bands: nonmagnetic metals.
d- and f- electron wave functions shrink as shell fills: electronic localization, magnetism.

## Slide 6
Cuprates
Heavy Electron Intermetallics
AF
SC
CePd2Si2
Mathur 1998
Organic Conductors
(Jaccard 2001)
Iron pnictides
Magnetic Order vs Superconductivity in Correlated Electron Systems

## Slide 7
…..one can also think about a phase transition in a zero-temperature system which occurs when, say, a coupling constant reaches a certain threshold. In this case, none of the fluctuation modes have thermal energies, and their statistics will be highly nonclassical.
------- John Hertz 1976
Quantum Critical Points (QCPs) Separate Different Phases at T=0
P, B, x

## Slide 8: YbRh2Si2: An Unconventional Metal near the Quantum Critical Point
Steglich 2002
(Custers 2003)
Unconventional metal near QC point (B=BQCP, T<10 K)
YbRh2Si2: Non-Fermi liquid metal r~r0+aT
Simple metal (Li): Fermi liquid metal r~ro+AT2
Near QCP: unconventional metals are the disordered states from which
new ordered states emerge.
r=r0+aTn
BQCP
FL
FL
nFL
T(K)
T2(K2)
Li
r-r0

## Slide 9: CeCu6-xAux: Quantum Critical Fluctuations Scaled by Temperature
XQCP=0.1
Inelastic neutron scattering experiments find that the dynamical susceptibility c”=c”(E/T), but in a Fermi liquid c”=c”(E/EF).
The only relevant energy scale for these quantum critical fluctuations is temperature itself.
Schroder 2000

## Slide 10
A Quantum Spin Liquid Near A QCP?
A Quantum Spin Liquid is a system with magnetic moments where
there are no broken symmetries.
It is a new state of matter found as T→0.
-The moments do not break translational symmetries, like a liquid.
-There is no magnetic order, which is suppressed by quantum fluctuations.
-It is not a paramagnet. Interactions lead to long-ranged entanglement of the wave functions.
The low energy properties of a Quantum Spin Liquid are related to effects such as:
-Quantum fluctuations
-Quantum entanglement
-Quantum coherence
-The topology of the quantum wave function.
The signature properties of a Quantum Spin Liquid are not fully known, but they include:
-Nonlocal and topological excitations.
-Fractionalized excitations.
QSL ground states may be topologically protected, suggesting possible role as qubits in quantum information applications.

## Slide 11
How to Discover a Quantum Spin Liquid?
Accessing a Quantum Critical Point GQCP (TN=0): Approaches for maximizing quantum fluctuations to disrupt order.
-Low Dimensionality
-Frustrated or Competing Interactions
-Singlet Formation (dimerization)
In metals, reducing the strength of correlations can destabilize magnetic moments (Kondo effect, Mott transition), weakening magnetic order.
TN
T
G (x,P,B)
GQCP
Thermal
Fluctuations
Quantum
Fluctuations
Ordering is a consequence of interactions J among moments: kBTC,N ~ zS(S+1) |J|
If J→0, the range of temperatures where you would see QC behavior shrinks as TC→0.
Paramagnet (disordered)
Ferromagnet (ordered)

## Slide 12
Triangular Lattice with AF near-neighbor interactions is inherently frustrated.
Huge ground state degeneracy → quantum fluctuations may be strong
Competing exchange interactions often lead to magnetic order.
A need to find new candidates for QSL.
1
2
3
4
5
6
Geometrical Frustration: Balance of Competing Interactions

## Slide 13
Kagome
Hyper-Kagome
A wealth of lattices with triangular motifs where frustration is important

## Slide 14
Noncollinear spins with Neel order. Broken rotational and time reversal symmetries.
Valence Bond State. Broken rotational symmetry, time reversal symmetry remains unbroken.
Quantum Critical Point
Ising Spins (Read 1991)
Heisenberg Spins
Fazekas and Anderson 1974
Jring/J (Motrunich 2005)
Conventional Magnetic Order vs Valence Bond State

## Slide 15
Spin liquid: no broken symmetries, massively entangled.
+
+
+
+….
Fazekas and Anderson 1974
Singlets in Valence Bond State vs Quantum Spin Liquid
Valence Bond State. Broken rotational symmetry, time reversal symmetry remains unbroken.

## Slide 16: Long Ranged Entanglement Required for Quantum Spin Liquid
An electron with charge e, spin S=1/2 on each lattice site
Each singlet: two charges e, S=0 singlet (|↑↓> - |↓↑>)/√2
Valence Bond Solid
Short Ranged Interactions
Broken rotational and translational symmetries
Resonating Valence Bond State
+
+
+ …
Long Ranged Entanglement of Singlets
No broken symmetries
At present, there are no viable Hamiltonians known that produce a Quantum Spin Liquid from RVB-like states.
Higher order interactions may tend to drive ordered configurations.
Different moment types, lattice symmetries, interaction types. QSL still an open question.
P. W. Anderson 1972

## Slide 17: Composite Electrons: Resonant Valence Bond State on a Square Lattice
Two quasiparticles created, but
no new charge. Each quasiparticle
S=1/2. They are spinons.
Ground State: Superposition of Singlets with
Long-ranged entanglement
Excited State: Break a Dimer Bond
Remove two charges: hole doping
Two delocalized holes form singlet S=0.
Together, holes have charge -2e
This quasiparticle is a holon.
Long-ranged entanglement of the electron wavefunction produces new excitations with spin, charge, and orbital associated
with individual electrons.
Resonating Valence Bond (RVB) state envisaged as normal state for unconventional superconductors (Anderson 1987).
The holons allow charge to be mobile in the RVB state, and their quantum entanglement would lead to superconductivity.

## Slide 18: Frustrated Magnetism + Unstable Moments → New Phases
Virtually all of the geometrically frustrated and low dimensional materials that are quantum spin liquids are insulating.
Introducing mobile charge that could lead to unconventional superconductivity is generally unsuccessful.
If metallic analogs of insulating systems with strong quantum fluctuations can be found, initial evidence suggests that proximity to an electronic instability such as the Mott transition may lead to new phases ,perhaps unconventional superconductivity.
What new ordered and disordered states will be found if magnetic moments themselves can be controlled?
Our research seeks new systems where the magnetism of d- and f-electrons is in transition, as is their ability to order.
Organic Conductor
k-(ET)2Cu2(CN)3
Kurosaki 2018

## Slide 19: Electronic Delocalization: Kondo Compensation of Magnetic Moments
T>>TK
Paramagnet
c~1/T
T~TK
Kondo singlet forms
T<<TK
Kondo singlet complete
Nonmagnetic metal c~1/TK
T/TK
c/c0
kBTK
Due to exchange coupling, the conduction electrons of a metal and the localized
f- or d- electron moments form a S=0 singlet.
The Kondo effect has a characteristic scale TK, separating paramagnetism
(T>>TK) and nonmagnetic metal (T<<TK).
The Kondo effect effectively delocalizes the magnetic d- or f-electron, and the
formation of the Kondo resonance increases the number of states contained in
The Fermi surface.

## Slide 20
Ground States with Localized or Delocalized d or f-electrons
Two ways to create a Quantum Critical Point where TC→0:
-frustrate magnetic interactions (no change in Fermi surface volume) Could happen in metals or insulators
-destroy the ordering moment (possible change in Fermi surface volume) Can only happen in metals
Temperature
J’
QCP
Small FS
f-electrons excluded
Large FS
f-electrons included
Magnetic Order
Localized electrons
No order (Fermi Liquid)
Delocalized electrons
J’
TK=0
TK>>TC

## Slide 21: A Global Phase Diagram for Correlated Electron Systems?
Increasing quantum fluctuations Q suppress T=0 magnetic order:
-Low dimensionality
-Geometrical frustration: triangular, Kagome, pyrochlore lattices.
- Dimerization: Shastry-Sutherland lattice.
Additional interplay of electronic delocalization G and order in correlated metals (Kondo and Mott Physics).
A need for new metallic and geometrically frustrated compounds to compare to benchmark insulators.
Q. Si, (2010)
P. Coleman & A. Nevidomskyy, (2010)
G (P,x)
T=0
GQCP
Magnetic Order
Spin Liquid
Q
Quantum Fluctuations
QQCP
Spin Liquid
Large
FS
Large FS
Small
FS
Small FS
SC?

## Slide 22
Strong fluctuations in low-dimensional magnets
Mermin-Wagner Theorem:
``In one and two dimensions, continuous symmetries cannot be broken at nonzero temperatures in
systems with sufficiently short-ranged interactions.’’
n
n+1
n+2
A chain with nearest –neighbor interactions J
a ± x
a ± x
a ± x
Since the atoms fluctuate independently:
Relative fluctuation between near neighbor atoms (n,n+1), or (n=1,n+2): ~x
Relative fluctuation between second neighbor atoms n, n+2: √2 x
The fluctuations become increasingly uncorrelated with the distance between atoms in one-dimensional systems. Correlations are short-ranged as in a liquid or gas, and do not persist on long length scales, as needed to drive a true phase transition.

## Slide 23
Fractionalized Excitations in Spin S=1/2 Chain: Spinons
Flip one spin relative to AF background (DS=1) `magnon’
Spinons: a fundamental excitation with S=1/2, charge = 0.
Spinons are found in spin chains, and in certain frustrated lattices.
The spinon carries the spin of the electron, but not its charge. It is `part of an electron’, ie a fractionalized particle.
The spinons are confined on chains, since the energy cost for the spinons grows linearly with their separation.
Spinon spectra can be studied using inelastic neutron scattering, as well as angle-resolved photoemission.
AF state is restored by generation of two spinons that propagate. Each carries half of flipped spin, so spinon S=1/2

## Slide 24: Yb2Pt2Pb: Spinons in Metallic Chains of Yb3+ Moments
3.545 Å
qAF-=(0.2,-0.2,0)rlu
qAF+=(0.2,0.2,0) rlu
d1
d2
d3
d1=3.545 Å
d2=3.965 Å
d3=3.889 Å
d4=3.510 Å
c-axis
d4
3.51 Å
3.889 Å
3.965 Å
Yb3+ moments with jZ=±7/2 doublet ground states form planes of orthogonal dimers in the Shastry-Sutherland Lattice (SSL).
Planes stack with closest Yb-Yb distance along c-axis: One dimensional magnetic system ``orthogonal spin ladders’’
Yb2Pt2Pb is an excellent metal, with weak coupling between conduction electrons, Yb moments. Small Fermi surface?
Weakly coupled Spin ladders
(Pöttgen 1999)

## Slide 25
Dispersing excitations along (00L): continuum of fractionalized S=1/2 quantum excitations .
Gapped, dispersionless excitations in the HHL (SSL) plane: excitations are confined to one-dimensional ladder rails.
Excitations have characteristic spinon dispersion expected for spin S=1/2 Ising-Heisenberg XXZ Hamiltonian:
T=0.1 K, B=0
Wu et al 2016
Yb2Pt2Pb: Fractionalized Quantum Excitations

## Slide 26
The Spinon Bandwidth: an Emergent Energy Scale
Doublet ground state |±7/2> = a↑|7/2> + a↓|-7/2>
Interactions that are bilinear in J (Zeeman, Heisenberg-Dirac exchange, dipolar) can only change quantum number DmJ=± 1,
so they have no matrix elements that would allow transitions within ground state wavefunction, which require DmJ=7.
Yb3+ moment: a 4f hole with orbital momentum L=3, |mL|=3 and 6-fold symmetry around J quantization axis.
A consequence of large energy scales: spin-orbit coupling, crystal fields, Coulomb interactions.
Orbital exchange: the permutation of neighboring electron orbitals |mJ1,mJ2> and |mJ2,mJ1> with equal weights, driven
by orbital overlap.
Hopping allowed
|DmJ|=7
Hopping blocked
mL=3
mL=-3
mL=3
mL=3

## Slide 27: A Global Phase Diagram for Correlated Electron Systems?
Q. Si, (2010)
P. Coleman & A. Nevidomskyy, (2010)
G (P,x)
T=0
GQCP
Magnetic Order
Spin Liquid
Q
Quantum Fluctuations
QQCP
Spin Liquid
Large
FS
Large FS
Small
FS
Small FS
SC?
Yb2Pt2Pb: a one-dimensional, metallic, spin liquid with localized moments

## Slide 28
Cr,Mn,Fe,Co
Bi
Ti
Richter 1997
a
b
7.5 Å
Well separated chains of Mn ions encased in Ti and Bi tubes:
Mn-Mn spacing: Interchain: 7.5Å Intrachain: 2.4 Å
Naturally located near moment formation in correlated band (Coey 2010)?
dMn-Mn ≤ 2.4 Å  nonmagnetic band (U/4t<1)
2.5 Å ≤ dMn-Mn ≤ 2.8 Å  emerging Mn moment, antiferromagnetic order
dMn-Mn ≥ 2.9 Å  Localized Mn moments, ferromagnetic order (U/4t>1)
Ti4MnBi2: Mn Moment Formation in a 1-D Chain?

## Slide 29
G
G+<1-10>
G
G+<1-10>
ARPES: 1D dimensional Fermi Surface in Ti4MnBi2
Utsuji 2013
45 K

## Slide 30
meff=1.79 mB/Mn (S=1/2)
q=-9.3 K (AF)
Curie-Weiss moment: mCW=1.79 mB/Mn (S=1/2) Low spin configuration.
Strong fluctuations make Mn valence and spin state ill-defined: broad band (-2.5eV to 2.5 eV).
Density of states dominated by Ti d-states, moderate correlations: Dg(EF)~3.4D(EF)DFT
Mn dx2-y2, dxy orbitals are spin polarized. AF order observed TN~1.9 K, but entropy is only ~10% of Rln2.
Ti4MnBi2: Quantum fluctuations from 1D and/or moment collapse?
Pandey 2020

## Slide 31: A Global Phase Diagram for Correlated Electron Systems?
Q. Si, (2010)
P. Coleman & A. Nevidomskyy, (2010)
G (P,x)
T=0
GQCP
Magnetic Order
Spin Liquid
Q
Quantum Fluctuations
QQCP
Spin Liquid
Large
FS
Large FS
Small
FS
Small FS
SC?
Yb2Pt2Pb: a one-dimensional, metallic, spin liquid with localized moments Small FS
Ti4MnBi2: a one-dimensional, metallic, (near) spin liquid with weak, itinerant moments Large FS